## Slide 1: Thermal Equilibrium and Non-Equilibrium in Composite Materials: A Comparison between DNS and Analytical Homogenization
, , ,
Institut de Mécanique et d Ingénierie de Bordeaux (I2M), Université de Bordeaux
Centre National de la Recherche Scientifique (CNRS)
Laboratoire Sols – Solides – Structures –Risque (3SR), Université de Grenoble-Alpes
Club Cast3M November 2025

## Slide 2
Introduction

## Slide 3: Introduction: State of Art
Video 1: X- ray/Neutron images of a drying concrete
sample. (S. Dal Pont 3SR)
Figure 1: Sample tomography and drying Evolution.
(M.H. Moreira et al. 2022, C.S. Hani et al. 2024)

## Slide 4: Introduction: Research Motivation
Figure 2: (A) TomoToFE Python pipeline: https://github.com/ANR-MultiFIRE/TomoToFE,
(C.S. Hani et al. 2024, 10.21809/rilemtechlett.2023.184 ). (B) Imported mesh on CAST3M .
(A)
(B)

## Slide 5: Introduction: Research Motivation
Figure 2: Snapshot of a shrinkage simulation with a THCM model on the imported mesh with CAST3M.
Video 2: Shrinkage simulation on the mesh exported from the bbbbb real sample.

## Slide 6
Introduction
Mathematical Model

## Slide 7: Mathematical Model: Meso-Scale Equations
Figure 3: Sketch of a porous medium including a sample of the averaging volume and the characteristic length-scales. D. Lasseux and F.J.Valdés-Parada2025. https://doi.org/10.1016/j.advwatres.2025.104899
Non Thermal Equilibrium;
Fourier’s Law applicability;
Neglecting the interfacial resistance to heat transfer.

## Slide 8: Mathematical Model: Volume Averaging Method (VAM)
Applying the intrinsic average operator
Separation of the length-scales: ;
The media is statiscally homogeneous at ;
The media is pseudo-periodic;
Spatial averaging theorems (Whitaker 1999, 10.1007/978-94-017-3389-2);
Decomposition (Gray 1975, https://doi.org/10.1016/0009-2509(75)80010-8);
Macroscopic Thermal Non - Equilibrium Equations

## Slide 9: Mathematical Model: Effective Coefficients
Dominant and Coupled
heat conductivity tensors
Dominant Conduction and Co-Conduction heat corrective vectors
Effective interfacial heat coefficient

## Slide 10: Mathematical Model: Properties of Effective Coefficients
As showen in D. Lasseux and F.J. Valdés-Parada 2025 (https://doi.org/10.1016/j.advwatres.2025.104899)

## Slide 11: Mathematical Model: Thermal Non - Equilibrium and Thermal Equilibrium
Macroscopic Thermal Non - Equilibrium Equations (2Eqs. Model)
Macroscopic Thermal Equilibrium Equation (1Eq. Model)

## Slide 12
Introduction
Mathematical Model
Numerical Simulations

## Slide 13: Numerical Simulations: Direct Numerical Simulation (DNS)
Figure 3: Sketch of the microscale domain considered for the DNS.

## Slide 14: Numerical Simulations: Direct Numerical Simulation (DNS)
Proposed CAST3M procedure

## Slide 15: Numerical Simulations: Closure Problems
Figure 5: Periodic and symmetric unit cell for the closure problems solution.
Figure 6: 2D - Periodic and symmetric unit cell for the closure problems.
Notes: By exploiting the symmetry of the unit cell, the three-dimensional closure problem can be reduced to a two-dimensional one in the – plane.
In this configuration, there is no flow along the -direction, and the -component of the normal vector is zero. Consequently, the problem reduces to a purely 2D formulation.
By exploiting the symmetry of the unit cell, the three-dimensional closure problem can be reduced to a two-dimensional one in the 𝑦–𝑧 plane.
In this configuration, there is no flow along the 𝑥-direction, and the 𝑥-component of the normal vector 𝐧 is zero. Consequently, the problem reduces to a purely 2D formulation.

## Slide 16: Numerical Simulations: Macroscopic Model
CAST3M procedure:
CHARTHER
Proposed CAST3M procedure:
diffu2.dgibi

## Slide 17: Numerical Simulations: Macroscopic Model
Figure 7: Macroscopic 1D representation of the considered geometry.
Macroscopic No-Thermal Equilibrium Equations (2Eqs. Model)

## Slide 18: Numerical Simulations: Summery
Microscale Equations (DNS)
Closure Problems
Macroscale Equations

## Slide 19: Numerical Simulations: Test Cases

## Slide 20: Numerical Simulations: DNS - Test Case LC -
Figure 8: Direct Numerical Simulation (DNS) at different time of for in LC-case.

## Slide 21: Numerical Simulations: DNS vs 2 Eqs. vs 1 Eq. - Test Case LC -
Figure 9: Comparison between Direct Numerical Simulation (DNS), 2Eqs. and 1 Eq. at different time of for in LC-case.

## Slide 22: Numerical Simulations: Test Cases

## Slide 23: Numerical Simulations: DNS - Test Case MC -
Figure 10: Direct Numerical Simulation (DNS) at different time of for in MC-case.

## Slide 24: Numerical Simulations: DNS vs 2 Eqs. vs 1 Eq. - Test Case MC -
Figure 11: Comparison between Direct Numerical Simulation (DNS), 2Eqs. and 1 Eq. at different time of for in MC-case.

## Slide 25: Numerical Simulations: Test Cases

## Slide 26: Numerical Simulations: DNS - Test Case HC -
Figure 12: Direct Numerical Simulation (DNS) at different time of for in HC-case.

## Slide 27: Numerical Simulations: DNS vs 2 Eqs. vs 1 Eq. - Test Case HC -
Figure 13: Comparison between Direct Numerical Simulation (DNS), 2Eqs. and 1 Eq. at different time of for in HC-case.

## Slide 28: Numerical Simulations: DNS vs 2 Eqs. vs 1 Eq. - Test Case HC -
Figure 14: Comparison between 1 Eq. model and at different time in HC-case.

## Slide 29
Introduction
Mathematical Model
Numerical Simulations
Conclusion

## Slide 30: Conclusion: Objectives Achieved and Future Perspectives
Estimation of the effective parameters;
Good agreement between DNS and homogenized model;
Assessment of the applicability of the two-equation vs one-equation model.
Relax the time constraint hypothesis (Unsteady macroscopic one and two-equation models for equilibrium and non-equilibrium diffusive process in heterogeneous media, IN PREPARATION) .
Promote the implementation of periodic boundary conditions in CAST3M to solve closure problems.