## Slide 1: An approach to thermomechanical modelling of welding and additive manufacturing in Cast3M
S. Pascal, DES/ISAS/DRMP/SRMA/LTA, CEA Saclay, France

## Slide 2: Introduction
  State of the art
    Numerical welding simulation uses finite element codes for structural analysis
    It takes benefit of decades of experience in thermomechanical modelling that have led to:
      Robust and proven numerical methods
      Performant nonlinear solvers
      Numerous mechanical behavior laws
      Accessible and validated material data
  However, modelling welding and additive manufacturing processes presents two specific characteristics:
    Mobile heat input, also variable in time
    Material deposition
Subject of today’s talk!

## Slide 3: Outlines
Mobile heat input
  Heat source models
  Spatiotemporal evolution
Material deposition
  Model geometry evolution
  Energy conservation
Applications

## Slide 4: Mobile heat input
  Heat source models: why?
    Heat input processes impose heat fluxes (electric arc, laser…)
    However:
    Thermal modelling of these processes uses heat source models to account for hydrodynamic effects in the molten pool
    Example: Goldak1 heat source model Good representation of the molten pool but 8 parameters to identify (at least)
  Heat source models in Cast3M
    Development of heat source models: MOD1 = MODE GEO1 THERMIQUE SOURCE… ;
    Two gaussian heat source models:
      … SOURCE GAUSSIENNE ELLIPTIQUE ;
      … SOURCE GAUSSIENNE ELARGIE ;
1J. Goldak, A. Chakravarti, M. Bibby. “A new finite element model for welding heat sources”, Metallurgical Transactions B, vol. 15, 299–305, 1984.
Goldak1 heat source model

## Slide 5: Mobile heat input
  “SOURCE GAUSSIENNE ELLIPTIQUE”
    “Basic” gaussian heat source model
    Thermal power density distribution function: space coordinates in local cylindrical frame of axis , and such that:
    5 parameters:
      : location and orientation
      : shape
      : power
Expression of for 3 calculation modes: plane, axisymmetric and tridimensional.

## Slide 6: Mobile heat input
  “SOURCE GAUSSIENNE ELARGIE”
    Simplified heat source model to represent sweep welding
    Thermal power density distribution function (only in 3D mode): space coordinates in local frame
    7 parameters:
      : location and orientation
      : shape
      : power

## Slide 7: Mobile heat input
  Mobile heat source modelling
    Based on:
      Heat source trajectory, modelled as an oriented meshed line (LTRAJ1)
      Time evolution of its displacement along this line (EVXS1)
    In Cast3M, definition of a CHARGEMENT type object: CHXS1 = LTRAJ1 COOR CURV ; CGXS1 = CHAR TRAJ CHXS1 EVXS1 ;
    Use for a given time TPS1: PTXS1 = TIRE CGXS1 TRAJ TPS1 ;
LTRAJ1
EVXS1
CHXS1
x
PTXS1

## Slide 8: Mobile heat input
  Mobile heat source modelling
    Connection to the heat source models in Cast3M: MODQS1 = MODE GEO1 THERMIQUE SOURCE GAUSSIENNE… ; MATQS1 = MATE MODQS1 ORIG CGXS1 QTOT EVQS1 RGAU RG1 ZGAU ZG1 DIRE NS1… ;
    the location of the heat source can be updated at any time by giving CGXS1, as well as the heat source intensity by giving EVQS1
EVQS1

## Slide 9: Outlines
Mobile heat input
  Heat source models
  Spatiotemporal evolution
Material deposition
  Model geometry evolution
  Energy conservation
Applications

## Slide 10: Material deposition
  Geometry evolution
    Basic idea: add blocks of finite elements du simulate material deposition
    In practice:
      Define as many mesh as there are geometries involved in the simulation
      At time , update the geometry according to the following rule:
    Data structure in Cast3M: create a list of meshes (LISTOBJE) and a timetable (LISTREEL): LGEO1 = ENUM GEO1 GEO2 GEO3 … GEOn ; LTPS1 = PROG t0 t1 t2 … tn ;
geometry GEO1
geometry GEO2
geometry GEOn

## Slide 11: Material deposition
  Model evolution
    Define as many models as there are meshes in LGEO1: LMOD1 = ENUM ; LMAT1 = ENUM ; REPE B1 (DIME LGEO1) ; GEOI1 = LGEO1 EXTR &B1 ; MODI1 = MODE GEOI1 MECANIQUE ELASTIQUE … ; MATI1 = MATE MODI1 YOUN YM1 NU NU1 … ; LMOD1 = LMOD1 ET MODI1 ; LMAT1 = LMAT1 ET MATI1 FIN B1 ; CGMOD1 = CHAR MODE LTPS1 LMOD1 ; CGMAT1 = CHAR MATE LTPS1 LMAT1 ;
    Use in PASAPAS input table: TAB1.MODELE = CGMOD1 ; TAB1.CARACTERISTIQUES = CGMAT1 ;
    During resolution, PASAPAS updates the model and its characteristics, which makes the geometry evolving.

## Slide 12: Material deposition
  Thermal analysis: temperature initialization during model change
    Temperature at interface ?  energy conservation
    where are the heat capacity matrices and the nodal temperatures.
    With:
    we get:
    Important remark: is temperature at the beginning of the next time step.
?

## Slide 13: Material deposition
  Mechanical analysis: displacements and stresses initialization during model change
    Static analysis: no mechanical energy in
    Displacement field at interface :
    Moreover:
    Initial stress free strain applied to the added part to cancel this input of mechanical energy:
?

## Slide 14: Outlines
Mobile heat input
  Heat source models
  Spatiotemporal evolution
Material deposition
  Model geometry evolution
  Energy conservation
Applications

## Slide 15: Applications
  Example of thermal analysis : tube manufacturing with WAAM process 1
TC-7
Time evolution of temperature (°C) at a thermocouple location
Time evolution of temperature node field (°C)
1S. Pascal, M. Garnier, M. Garric, J. Le Mercier. Modélisation thermomécanique de la fabrication additive arc-fil d’un tube droit avec Cast3M, 16ieme Colloque National en Calcul des Structures (CSMA 2024), CNRS, CSMA, ENS Paris-Saclay, CentraleSupélec, mai 2024, Hyères, France.

## Slide 16: Applications
  Example of mechanical analysis : wall manufacturing with WAAM process1,2
Time evolution of displacement (mm) at the plate end
Time evolution of von Mises stress field (MPa)
exe
Experimental measure
Linear isotropic hardening, large displacement analysis
1C. Cambon, S. Rouquette, I. Bendaoud, C. Bordreuil, R. Wimpory, F. Soulié. Thermo-mechanical simulation of overlaid layers made with Wire + Arc Additive Manufacturing and GMAW-Cold Metal Transfer, Welding in the World, Vol. 64 No. 8, pp 1427-1435.
2S. Pascal, S. Gounand. Modélisation thermomécanique d’un cas d’étude de fabrication additive arc-fil,15ieme Colloque National en Calcul des Structures (CSMA 2022), Université Polytechnique Hauts-de-France, [UPHF], mai 2022, Hyères, France.

## Slide 17: Applications
  Example of mechanical analysis : wall manufacturing with WAAM process1
1D. Artieres. Microstructure et propriétés de l’acier 316L élaboré par fabrication additive par dépôt de fil (WAAM & WLAM) : caractérisation expérimentale et modélisation, thèse de doctorat, Université Paris sciences et lettres, 2025.

## Slide 18: Merci de votre attention
CEA SACLAY
91191 Gif-sur-Yvette Cedex
France
serge.pascal@cea.fr
Standard. + 33 1 69 08 60 00